Figure S1: Plasticity chart, for Xi, Koutala, Matzavinata and Chavdata lo-cations.

Figure S2: Plasticity chart, for Arillas and Ag. Stefanos locations.

Figure S3: Kefalonia Is-land. Xi and Matzavinata thermogravimetric analysis (TGA).

Figure S4: Kefalonia Island. Xi and Matzavinata Thermal Analysis.

Figure S5: Corfu Island. Ag. Stefanos thermogravimetric analysis (TGA).

Figure S6: Corfu Island. Thermal analysis of Ag. Stefanos samples.

Supplementary Tables

Table S1: Chemical analysis for trace elements results.

| Location | Samples | mg/Kg in dry matter |
| --- | --- | --- |
|  | Li | Be | V | Cr | Mn | Co | Ni | Cu | Zn | Ga | As | Rb | Sr | Mo | Ag | Cd | Te | Ba | Pb | U | Bi |
| toxic limits [32] | 50-75? | 2 to 6 | 80-130 | 80-120 |  | 14-20 | 40-90 | 40-60 |  | 19-25 | 13 | 120-200 | 300-450 | 2-2.6 | 0.007 | 0.3 |  | 500-800 | 20-40 | 3 to 4 | 0.05-0.40 |
| toxic limits [33] |  |  |  | 1100 |  | 5 | 60 | 130 |  |  | <8 |  |  | 18 | 17 | 3 |  | 1300 | <50 |  |  |
| in earth muds | 50-75 | 2 to 6 | 80-130 | 80-120 | 400 - 850 | 14-20 | 40-90 | 40-60 | 80-120 | 15-25 | 15-13 | 120-200 | 300-450 | 2-2.5 | 0.07-0.1 | 0.5-0.7 | 0.02-0.7 | 147-248 or 500-800 | 14-40 | 3 to 4 | 0.05-0.5 |
| Xi beach/Kefalonia | X10 | 36 | 3 | 62 | 94 | 455 | 14 | 97 | 21 | 54 | 17 | 4 | 55 | 200 | 2 | <1 | <1 | 2 | 180 | 9 | 1 | <1 |
|  | X11 | 58 | 2 | 84 | 145 | 595 | 18 | 116 | 24 | 67 | 21 | 6 | 71 | 540 | 3 | <1 | <1 | <1 | 210 | 11 | 2 | <1 |
|  | X12 | 70 | 2 | 98 | 140 | 595 | 19 | 126 | 29 | 86 | 27 | 7 | 90 | 260 | 3 | <1 | <1 | <1 | 260 | 15 | 2 | <1 |
|  | X13 | 81 | 2 | 125 | 170 | 635 | 22 | 160 | 34 | 94 | 31 | 7 | 107 | 240 | 7 | <1 | <1 | <1 | 280 | 17 | 2 | <1 |
|  | X14 | 73 | 2 | 125 | 165 | 645 | 22 | 155 | 35 | 102 | 27 | 5 | 91 | 210 | 6 | <1 | <1 | <1 | 230 | 14 | 2 | <1 |
|  | X15 | 79 | 2 | 115 | 160 | 650 | 22 | 155 | 32 | 89 | 27 | 6 | 99 | 240 | 7 | <1 | <1 | <1 | 230 | 13 | 2 | <1 |
|  | X16 | 77 | 2 | 120 | 200 | 680 | 22 | 174 | 37 | 92 | 28 | 5 | 102 | 220 | 5 | <1 | <1 | <1 | 240 | 14 | 2 | <1 |
|  | X17 | 63 | 2 | 94 | 130 | 700 | 19 | 125 | 29 | 91 | 27 | 9 | 100 | 290 | 3 | <1 | <1 | <1 | 280 | 13 | 2 | <1 |
|  | X19 | 61 | 2 | 94 | 145 | 650 | 19 | 137 | 25 | 88 | 23 | 5 | 72 | 230 | 3 | <1 | <1 | <1 | 220 | 11 | 1 | <1 |
|  | X19 | 55 | 2 | 76 | 140 | 580 | 16 | 140 | 25 | 73 | 24 | 6 | 67 | 250 | 6 | <1 | <1 | <1 | 250 | 12 | 2 | <1 |
|  | X21 | 49 | 2 | 68 | 110 | 485 | 15 | 106 | 32 | 65 | 19 | 7 | 62 | 430 | 3 | <1 | <1 | <1 | 190 | 9 | 2 | <1 |
|  | X22 | 67 | 2 | 96 | 145 | 570 | 19 | 140 | 28 | 80 | 24 | 5 | 84 | 235 | 4 | <1 | <1 | <1 | 230 | 11 | 2 | <1 |
|  | X23 | 39 | 1 | 54 | 81 | 505 | 13 | 79 | 14 | 50 | 17 | 5 | 49 | 330 | 1 | <1 | <1 | <1 | 170 | 8 | 1 | <1 |
|  | X24 | 58 | 1 | 85 | 145 | 560 | 17 | 135 | 26 | 72 | 22 | 6 | 77 | 250 | 4 | <1 | <1 | <1 | 210 | 13 | 2 | <1 |
|  | X25 | 57 | 1 | 88 | 140 | 540 | 18 | 120 | 27 | 75 | 23 | 6 | 79 | 270 | 2 | <1 | <1 | <1 | 230 | 12 | 1 | <1 |
|  | X26 | 58 | 2 | 90 | 13 | 560 | 18 | 120 | 26 | 77 | 23 | 5 | 80 | 280 | 2 | <1 | <1 | <1 | 220 | 10 | 2 | <1 |
|  | X27 | 58 | 2 | 92 | 130 | 560 | 18 | 130 | 34 | 75 | 24 | 5 | 75 | 225 | 6 | <1 | <1 | <1 | 220 | 12 | 2 | <1 |
|  | X28 | 60 | 1 | 92 | 135 | 570 | 17 | 125 | 28 | 74 | 23 | 4 | 78 | 210 | 6 | <1 | <1 | <1 | 220 | 11 | 2 | <1 |
|  | X29 | 58 | 1 | 85 | 135 | 545 | 17 | 130 | 30 | 70 | 24 | 6 | 75 | 260 | 4 | <1 | <1 | <1 | 240 | 13 | 2 | <1 |
|  | X30 | 48 | 2 | 73 | 110 | 630 | 16 | 110 | 24 | 64 | 20 | 7 | 64 | 375 | 2 | <1 | <1 | <1 | 180 | 9 | 1 | <1 |
|  | X31 | 62 | 2 | 105 | 135 | 745 | 21 | 140 | 34 | 86 | 25 | 8 | 87 | 250 | 1 | <1 | <1 | <1 | 220 | 12 | 1 | <1 |
|  | X32 | 62 | 1 | 100 | 130 | 595 | 19 | 130 | 27 | 83 | 24 | 5 | 83 | 220 | 6 | <1 | <1 | <1 | 230 | 11 | 2 | <1 |
|  | X33 | 63 | 2 | 95 | 135 | 595 | 18 | 140 | 30 | 86 | 24 | 4 | 83 | 210 | 11 | <1 | <1 | <1 | 230 | 10 | 2 | <1 |
|  | X34 | 54 | 2 | 85 | 125 | 580 | 17 | 120 | 27 | 78 | 22 | 8 | 72 | 250 | 2 | <1 | <1 | <1 | 230 | 13 | 1 | <1 |
|  | X35 | 52 | 2 | 84 | 110 | 645 | 18 | 115 | 25 | 70 | 22 | 12 | 72 | 265 | 1 | <1 | <1 | <1 | 220 | 12 | 1 | <1 |
|  | X36 | 52 | 2 | 89 | 120 | 605 | 18 | 120 | 27 | 82 | 21 | 5 | 75 | 240 | 1 | <1 | <1 | <1 | 200 | 10 | 1 | <1 |
|  | X37 | 46 | 2 | 72 | 98 | 550 | 16 | 100 | 22 | 64 | 19 | 5 | 65 | 240 | 1 | <1 | <1 | <1 | 185 | 9 | 1 | <1 |
|  | X38 | 51 | 2 | 84 | 120 | 530 | 16 | 115 | 25 | 66 | 21 | 8 | 75 | 210 | 2 | <1 | <1 | <1 | 200 | 10 | 1 | <1 |
|  | X39 | 54 | 2 | 85 | 165 | 570 | 17 | 130 | 26 | 68 | 24 | 7 | 76 | 220 | 2 | <1 | <1 | <1 | 240 | 14 | 1 | <1 |
|  | X40 | 46 | 2 | 70 | 105 | 520 | 15 | 110 | 22 | 62 | 21 | 5 | 64 | 200 | 1 | <1 | <1 | <1 | 220 | 11 | 1 | <1 |
|  | X41 | 53 | 2 | 85 | 130 | 470 | 16 | 110 | 29 | 84 | 29 | 7 | 100 | 180 | 1 | <1 | <1 | <1 | 190 | 15 | 2 | <1 |
|  | X42 | 55 | 2 | 93 | 135 | 585 | 19 | 130 | 28 | 78 | 23 | 14 | 85 | 240 | 1 | <1 | <1 | <1 | 210 | 11 | 1 | <1 |
|  | X43 | 54 | 2 | 89 | 175 | 570 | 18 | 150 | 38 | 76 | 23 | 9 | 81 | 230 | 5 | <1 | <1 | <1 | 230 | 14 | 1 | <1 |
|  | X44 | 49 | 2 | 81 | 245 | 550 | 17 | 170 | 28 | 68 | 20 | 4 | 74 | 270 | 6 | <1 | <1 | <1 | 190 | 10 | 1 | <1 |
|  | X45 | 47 | 2 | 79 | 175 | 515 | 16 | 130 | 24 | 65 | 19 | 6 | 69 | 300 | 4 | <1 | <1 | <1 | 190 | 10 | 1 | <1 |
|  | X46 | 44 | 2 | 71 | 170 | 560 | 15 | 130 | 21 | 63 | 19 | 4 | 63 | 210 | 17 | <1 | <1 | <1 | 200 | 7 | 3 | <1 |
|  | X47 | 47 | 3 | 71 | 155 | 490 | 16 | 130 | 24 | 91 | 26 | 9 | 145 | 345 | 4 | <1 | <1 | <1 | 290 | 16 | 2 | <1 |
|  | X48 | 48 | 2 | 77 | 170 | 495 | 16 | 140 | 27 | 67 | 19 | 5 | 70 | 310 | 3 | <1 | <1 | <1 | 180 | 9 | 1 | <1 |
|  | X49 | 48 | 2 | 75 | 125 | 555 | 16 | 115 | 21 | 75 | 20 | 6 | 69 | 320 | 3 | <1 | <1 | <1 | 190 | 10 | 1 | <1 |
|  | X50 | 46 | 2 | 73 | 290 | 495 | 18 | 175 | 26 | 68 | 20 | 3 | 71 | 270 | 6 | <1 | <1 | <1 | 210 | 9 | 1 | <1 |
|  | X51 | 51 | 3 | 82 | 175 | 480 | 16 | 140 | 28 | 82 | 23 | 5 | 122 | 230 | 16 | <1 | <1 | 2 | 220 | 19 | 3 | <1 |
|  | X53 | 48 | 2 | 78 | 140 | 555 | 16 | 130 | 23 | 67 | 22 | 6 | 70 | 270 | 3 | <1 | <1 | <1 | 220 | 12 | 1 | <1 |
|  | X71 | 40 | 2 | 43 | 53 | 545 | 7 | 135 | 21 | 75 | 20 | 8 | 5 | 310 | 4 | <1 | <1 | <1 | 190 | 6 | 2 | <1 |
| Koutala beach/Kefalonia | Κ0 | 50 | 2 | 96 | 135 | 600 | 18 | 125 | 28 | 81 | 21 | 6 | 75 | 215 | 1 | <1 | <1 | <1 | 160 | 10 | 1 | <1 |
|  | Κ1 | 39 | 2 | 71 | 100 | 570 | 14 | 90 | 17 | 54 | 17 | 6 | 57 | 400 | 3 | <1 | <1 | <1 | 160 | 8 | 1 | <1 |
|  | Κ3 | 48 | 2 | 86 | 120 | 565 | 17 | 120 | 23 | 66 | 21 | 6 | 73 | 280 | 2 | <1 | <1 | <1 | 190 | 10 | 2 | <1 |
|  | Κ4 | 44 | 2 | 79 | 130 | 595 | 18 | 120 | 27 | 66 | 20 | 4 | 65 | 310 | 1 | <1 | <1 | <1 | 200 | 8 | 1 | <1 |
|  | Κ5 | 53 | 3 | 90 | 125 | 510 | 17 | 120 | 25 | 71 | 21 | 4 | 81 | 220 | 2 | <1 | <1 | <1 | 190 | 9 | 1 | <1 |
|  | Κ6 | 49 | 3 | 83 | 120 | 520 | 16 | 110 | 21 | 67 | 19 | 6 | 67 | 270 | 2 | <1 | <1 | <1 | 160 | 9 | 1 | <1 |
|  | Κ8 | 57 | 3 | 110 | 140 | 510 | 20 | 135 | 31 | 86 | 23 | 8 | 89 | 200 | 1 | <1 | <1 | <1 | 180 | 11 | 1 | <1 |
| Matzavinata/Kefalonia | ΜΑ1 | 43 | 3 | 71 | 110 | 510 | 16 | 105 | 22 | 61 | 20 | 8 | 63 | 255 | 2 | <1 | <1 | 2 | 220 | 12 | 2 | <1 |
|  | ΜΑ2 | 42 | 2 | 72 | 100 | 545 | 16 | 105 | 22 | 59 | 19 | 9 | 64 | 230 | 1 | <1 | <1 | 2 | 200 | 11 | 1 | <1 |
|  | ΜΑ3 | 44 | 3 | 71 | 120 | 540 | 15 | 105 | 23 | 85 | 24 | 14 | 165 | 255 | 1 | <1 | <1 | 2 | 270 | 12 | 2 | <1 |
|  | ΜΑ4 | 46.6 | 3 | 80 | 115 | 600 | 17 | 110 | 25 | 78 | 24 | 15 | 142 | 220 | 1 | <1 | <1 | 2 | 260 | 12 | 2 | <1 |
|  | ΜΑ5 | 45 | 2 | 82 | 120 | 555 | 17 | 116 | 27 | 65 | 21 | 5 | 74 | 225 | 2 | <1 | <1 | 2 | 210 | 10 | 1 | <1 |
|  | ΜΑ6 | 38 | 2 | 66 | 87 | 475 | 14 | 95 | 21 | 54 | 17 | 4 | 62 | 240 | 1 | <1 | <1 | 2 | 180 | 9 | 1 | <1 |
|  | ΜΑ7 | 28 | 2 | 44 | 71 | 360 | 10 | 70 | 14 | 44 | 12 | 3 | 44 | 235 | 1 | <1 | <1 | 2 | 135 | 6 | 1 | <1 |
|  | ΜΑ8 | 43 | 3 | 72 | 105 | 555 | 15 | 100 | 21 | 61 | 20 | 12 | 67 | 235 | 2 | <1 | <1 | 2 | 220 | 10 | 2 | <1 |
|  | ΜΑ9 | 46 | 4 | 82 | 120 | 565 | 17 | 120 | 25 | 19 | 25 | 12 | 157 | 210 | 1 | <1 | <1 | 2 | 270 | 13 | 2 | <1 |
|  | ΜΑ10 | 31 | 2 | 76 | 105 | 480 | 15 | 105 | 24 | 75 | 16 | 6 | 52 | 180 | 2 | <1 | <1 | 2 | 140 | 10 | 1 | <1 |
|  | ΜΑ11 | 47 | 3 | 80 | 110 | 560 | 17 | 110 | 26 | 64 | 20 | 4 | 71 | 255 | 2 | <1 | <1 | <1 | 200 | 10 | 2 | <1 |
|  | ΜΑ12 | 33 | 2 | 57 | 86 | 465 | 14 | 88 | 17 | 56 | 17 | 9 | 60 | 330 | 2 | <1 | <1 | 2 | 190 | 9 | 1 | <1 |
|  | ΜΑ13 | 34 | 3 | 53 | 95 | 380 | 12 | 82 | 15 | 48 | 16 | 3 | 51 | 340 | 2 | <1 | <1 | 2 | 170 | 7 | 2 | <1 |
|  | ΜΑ14 | 30 | 2 | 49 | 76 | 395 | 13 | 75 | 13 | 50 | 14 | 4 | 45 | 400 | 1 | <1 | <1 | 2 | 150 | 6 | 2 | <1 |
|  | ΜΑ15 | 49 | 3 | 92 | 125 | 480 | 18 | 124 | 26 | 70 | 21 | 4 | 80 | 160 | 6 | <1 | <1 | 2 | 180 | 10 | 2 | <1 |
| Chavdata/Kefalonia | CH1 | 60 | 2 | 75 | 125 | 610 | 17 | 120 | 23 | 67 | 22 | 7 | 74 | 380 | 10 | <1 | <1 | <1 | 190 | 20 | 1 | <1 |
|  | CH2 | 51 | 3 | 93 | 155 | 590 | 18 | 145 | 35 | 82 | 22 | 7 | 82 | 205 | 4 | <1 | <1 | 2 | 200 | 13 | 1 | <1 |
|  | CH3 | 56 | 3 | 105 | 165 | 585 | 19 | 150 | 32 | 99 | 46 | 6 | 80 | 200 | 2 | <1 | <1 | 2 | 180 | 19 | 2 | <1 |
|  | CH4 | 48 | 3 | 77 | 270 | 645 | 19 | 190 | 26 | 65 | 21 | 17 | 72 | 310 | 4 | <1 | <1 | <1 | 220 | 12 | 1 | <1 |
|  | CH5 | 47 | 3 | 66 | 99 | 535 | 16 | 100 | 18 | 95 | 24 | 12 | 168 | 440 | 1 | <1 | <1 | 2 | 280 | 12 | 2 | <1 |
|  | CH6 | 46 | 3 | 73 | 110 | 540 | 16 | 110 | 22 | 62 | 18 | 6 | 67 | 350 | 3 | <1 | <1 | 2 | 180 | 10 | 1 | <1 |
|  | CH7 | 51 | 3 | 78 | 140 | 545 | 18 | 125 | 19 | 67 | 20 | 5 | 76 | 330 | 2 | <1 | <1 | 2 | 200 | 9 | 2 | <1 |
|  | CH8 | 42 | 3 | 84 | 125 | 535 | 17 | 120 | 24 | 75 | 18 | 5 | 71 | 270 | 3 | <1 | <1 | 2 | 150 | 13 | 1 | <1 |
|  | CH9 | 48 | 3 | 93 | 150 | 635 | 18 | 145 | 35 | 86 | 20 | 9 | 81 | 190 | 2 | <1 | <1 | 2 | 160 | 11 | 1 | <1 |
|  | CH10 | 42 | 3 | 91 | 120 | 490 | 16 | 120 | 26 | 69 | 9 | 9 | 68 | 180 | 2 | <1 | <1 | <1 | 140 | 10 | 1 | <1 |
|  | CH12 | 50 | 3 | 94 | 125 | 510 | 17 | 120 | 27 | 74 | 21 | 5 | 79 | 200 | 3 | <1 | <1 | <1 | 180 | 9 | 2 | <1 |
|  | CH14 | 50 | 3 | 95 | 140 | 500 | 17 | 130 | 27 | 83 | 20 | 7 | 73 | 210 | 2 | <1 | <1 | <1 | 160 | 10 | 1 | <1 |
|  | CH15 | 49 | 2 | 100 | 135 | 550 | 18 | 120 | 27 | 74 | 22 | 9 | 76 | 240 | 2 | <1 | <1 | <1 | 185 | 11 | 1 | <1 |
|  | CH17 | 49 | 2 | 90 | 130 | 600 | 18 | 120 | 23 | 75 | 20 | 5 | 80 | 320 | 2 | <1 | <1 | <1 | 150 | 9 | 1 | <1 |
|  | CH18 | 50 | 1 | 85 | 115 | 590 | 18 | 115 | 21 | 71 | 20 | 6 | 72 | 350 | 1 | <1 | <1 | <1 | 170 | 9 | 1 | <1 |
| Arillas beach/Corfu | Β2 | 58 | 3 | 85 | 165 | 720 | 20 | 160 | 30 | 69 | 20 | 4 | 74 | 530 | 5 | <1 | <1 | 2 | 210 | 11 | 2 | <1 |
|  | Β3 | 60 | 3 | 91 | 220 | 600 | 22 | 210 | 42 | 80 | 21 | 3 | 82 | 480 | 8 | <1 | <1 | 2 | 210 | 13 | 2 | <1 |
|  | Β4 | 51 | 3 | 83 | 210 | 810 | 22 | 220 | 33 | 81 | 22 | 4 | 69 | 555 | 9 | <1 | <1 | 2 | 270 | 13 | 1 | <1 |
|  | Β5 | 57 | 3 | 90 | 230 | 675 | 22 | 230 | 34 | 110 | 27 | 4 | 80 | 410 | 8 | <1 | <1 | 2 | 220 | 13 | 2 | <1 |
|  | Β6 | 54 | 2 | 94 | 240 | 700 | 24 | 270 | 36 | 86 | 27 | 6 | 94 | 455 | 11 | <1 | <1 | <1 | 300 | 12 | 1 | <1 |
|  | Β7 | 50 | 3 | 79 | 205 | 645 | 20 | 215 | 27 | 64 | 21 | 3 | 71 | 470 | 8 | <1 | <1 | 2 | 240 | 10 | 2 | <1 |
|  | Β8 | 49 | 2 | 78 | 190 | 845 | 21 | 220 | 34 | 69 | 21 | 7 | 70 | 550 | 8 | <1 | <1 | 2 | 230 | 14 | 2 | <1 |
|  | Β9 | 49 | 2 | 83 | 215 | 715 | 20 | 190 | 27 | 65 | 20 | 4 | 72 | 520 | 8 | <1 | <1 | 2 | 210 | 9 | 1 | <1 |
|  | Β10 | 49 | 2 | 84 | 175 | 595 | 21 | 190 | 32 | 75 | 23 | 5 | 75 | 378 | 3 | <1 | <1 | <1 | 250 | 12 | 1 | <1 |
|  | Β11 | 53 | 2 | 84 | 180 | 580 | 20 | 200 | 29 | 70 | 22 | 3 | 76 | 485 | 7 | <1 | <1 | 2 | 230 | 15 | 2 | <1 |
|  | Β12 | 50 | 2 | 87 | 185 | 650 | 18 | 190 | 32 | 76 | 21 | 5 | 60 | 330 | 7 | <1 | <1 | <1 | 230 | 10 | 2 | <1 |
|  | Β15 | 49 | 2 | 79 | 165 | 655 | 19 | 150 | 25 | 66 | 22 | 4 | 71 | 475 | 4 | <1 | <1 | <1 | 250 | 10 | 2 | <1 |
|  | Β17 | 51 | 2 | 83 | 160 | 553 | 19 | 170 | 29 | 69 | 23 | 4 | 75 | 380 | 5 | <1 | <1 | 2 | 260 | 10 | 2 | <1 |
|  | Β19 | 51 | 2 | 86 | 165 | 625 | 20 | 180 | 28 | 74 | 24 | 4 | 70 | 360 | 2 | <1 | <1 | <1 | 270 | 11 | 2 | <1 |
|  | Β21 | 44 | 2 | 79 | 155 | 790 | 19 | 160 | 28 | 72 | 22 | 4 | 61 | 340 | 2 | <1 | <1 | <1 | 250 | 10 | 2 | <1 |
|  | Β22 | 57 | 3 | 81 | 150 | 520 | 21 | 160 | 28 | 73 | 21 | 4 | 70 | 285 | 3 | <1 | <1 | 2 | 230 | 12 | 2 | <1 |
|  | Β31 | 40 | 2 | 73 | 180 | 530 | 21 | 160 | 23 | 64 | 22 | 4 | 61 | 350 | 2 | <1 | <1 | 2 | 270 | 9 | 2 | <1 |
|  | Β33 | 33 | 2 | 70 | 140 | 555 | 26 | 165 | 24 | 62 | 24 | 4 | 63 | 345 | 1 | <1 | <1 | 2 | 300 | 12 | 2 | <1 |
|  | Β39 | 38 | 2 | 79 | 155 | 530 | 22 | 170 | 26 | 67 | 25 | 4 | 63 | 430 | 2 | <1 | <1 | <1 | 320 | 10 | 2 | <1 |
|  | Β41 | 33 | 3 | 65 | 145 | 590 | 22 | 190 | 24 | 60 | 24 | 8 | 55 | 290 | 2 | <1 | <1 | 2 | 320 | 10 | 2 | <1 |
| Agios Stefanos beach/Corfu | Α0 | 60 | <1 | 90 | 180 | 590 | 21 | 210 | 36 | 110 | 26 | 4 | 83 | 330 | 2 | <1 | <1 | <1 | 290 | 10 | 2 | <1 |
|  | Α1 | 53 | <1 | 78 | 160 | 650 | 20 | 180 | 28 | 95 | 20 | 5 | 65 | 340 | 2 | <1 | <1 | <1 | 210 | 10 | 2 | <1 |
|  | Α2' | 62 | <1 | 98 | 210 | 690 | 23 | 230 | 39 | 98 | 24 | 6 | 84 | 315 | 3 | <1 | <1 | <1 | 250 | 12 | 2 | <1 |
|  | Α4 | 68 | 1 | 100 | 215 | 680 | 24 | 250 | 37 | 100 | 44 | 5 | 92 | 327 | 3 | <1 | <1 | <1 | 610 | 14 | 2 | <1 |
|  | Α5 | 61 | 1 | 90 | 180 | 640 | 21 | 190 | 30 | 99 | 24 | 5 | 78 | 358 | 2 | <1 | <1 | <1 | 240 | 14 | 2 | <1 |
|  | Α6 | 54 | <1 | 91 | 170 | 760 | 18 | 180 | 29 | 99 | 23 | 6 | 71 | 517 | 3 | <1 | <1 | <1 | 245 | 13 | 2 | <1 |
|  | Α7 | 55 | 2 | 100 | 200 | 680 | 24 | 215 | 35 | 130 | 20 | 7 | 82 | 320 | 1 | <1 | <1 | <1 | 220 | 14 | 2 | <1 |
|  | Α8 | 55 | 2 | 105 | 220 | 720 | 24 | 250 | 33 | 140 | 37 | 6 | 100 | 290 | 2 | <1 | <1 | <1 | 240 | 24 | 2 | <1 |
|  | Α9 | 60 | 2 | 110 | 210 | 940 | 25 | 230 | 33 | 95 | 27 | 5 | 92 | 300 | 2 | <1 | <1 | <1 | 275 | 14 | 2 | <1 |
|  | Α10 | 61 | 3 | 100 | 210 | 620 | 24 | 220 | 32 | 98 | 25 | 6 | 85 | 310 | 2 | <1 | <1 | 1.5 | 250 | 13 | 2 | <1 |
|  | Α11 | 59 | 3 | 105 | 205 | 640 | 25 | 230 | 94 | 28 | 19 | 19 | 105 | 340 | 3 | <1 | <1 | 2 | 305 | 15 | 2 | <1 |
|  | Α12 | 60 | 3 | 105 | 215 | 630 | 26 | 240 | 32 | 86 | 27 | 4 | 114 | 350 | 1 | <1 | <1 | <1 | 220 | 15 | 2 | <1 |
|  | Α13 | 56 | 3 | 100 | 210 | 705 | 23 | 230 | 34 | 97 | 28 | 9 | 83 | 270 | 2 | <1 | <1 | <1 | 320 | 16 | 2 | <1 |
|  | Α14 | 55 | 2 | 88 | 170 | 640 | 23 | 205 | 29 | 79 | 24 | 8 | 80 | 310 | 3 | <1 | <1 | <1 | 265 | 15 | 2 | <1 |
|  | Α15 | 63 | 3 | 97 | 190 | 630 | 23 | 210 | 30 | 100 | 24 | 4 | 82 | 330 | 1 | <1 | <1 | <1 | 255 | 11 | 2 | <1 |
|  | Α16 | 62 | 2 | 100 | 220 | 600 | 26 | 240 | 34 | 93 | 31 | 7 | 93 | 323 | 2 | <1 | <1 | <1 | 365 | 17 | 2 | <1 |
|  | Α17 | 50 | 2 | 86 | 170 | 570 | 21 | 180 | 29 | 80 | 22 | 4 | 73 | 300 | 1 | <1 | <1 | <1 | 230 | 11 | 2 | <1 |
|  | Α18 | 50 | 2 | 82 | 160 | 510 | 19 | 175 | 29 | 77 | 22 | 6 | 74 | 320 | 2 | <1 | <1 | <1 | 240 | 13 | 2 | <1 |
|  | Α19 | 48 | 2 | 84 | 160 | 555 | 20 | 170 | 24 | 74 | 21 | 4 | 74 | 450 | 1 | <1 | <1 | <1 | 235 | 13 | 2 | <1 |
|  | Α20 | 55 | 3 | 96 | 185 | 560 | 22 | 200 | 30 | 81 | 24 | 11 | 81 | 310 | 2 | <1 | <1 | 2 | 255 | 13 | 2 | <1 |

Table S2: Major elements results.

| Location | Samples | SiO2 | TiO2 | Al2O3 | tFe2O3 | MnO | MgO | CaO | Na2O | K2O | P2O5 | Total |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Xi beach/Kefalonia | Χ10 | 42,40 | 0,63 | 10,79 | 6,20 | 0,11 | 4,55 | 19,46 | 1,43 | 2,28 | 0,11 | 87,96 |
|  | X11 | 37,30 | 0,59 | 9,84 | 5,41 | 0,11 | 3,72 | 26,00 | 1,13 | 2,19 | 0,10 | 86,39 |
|  | X12 | 44,09 | 0,69 | 11,99 | 6,47 | 0,10 | 4,60 | 18,67 | 1,25 | 2,51 | 0,11 | 90,48 |
|  | X13 | 47,15 | 0,74 | 13,75 | 7,28 | 0,11 | 5,17 | 14,73 | 1,38 | 2,88 | 0,11 | 93,30 |
|  | X14 | 47,74 | 0,74 | 13,64 | 7,23 | 0,11 | 5,24 | 14,00 | 1,55 | 2,83 | 0,11 | 93,19 |
|  | X15 | 47,11 | 0,71 | 13,03 | 6,88 | 0,10 | 5,18 | 14,81 | 1,68 | 2,64 | 0,11 | 92,25 |
|  | X16 | 47,58 | 0,74 | 13,42 | 7,39 | 0,11 | 5,18 | 14,42 | 1,18 | 2,78 | 0,11 | 92,91 |
|  | X17 | 43,12 | 0,66 | 11,41 | 6,21 | 0,12 | 4,37 | 18,26 | 1,43 | 2,41 | 0,10 | 88,09 |
|  | X18 | 44,22 | 0,69 | 11,54 | 6,31 | 0,11 | 4,60 | 16,91 | 1,48 | 2,26 | 0,12 | 88,24 |
|  | X19 | 45,12 | 0,64 | 10,75 | 5,48 | 0,10 | 4,06 | 16,79 | 1,66 | 2,07 | 0,10 | 86,77 |
|  | X21 | 37,57 | 0,59 | 9,32 | 5,08 | 0,09 | 3,94 | 25,78 | 1,29 | 1,93 | 0,09 | 85,68 |
|  | X22 | 45,23 | 0,69 | 12,19 | 6,40 | 0,10 | 4,74 | 17,33 | 1,38 | 2,49 | 0,13 | 90,68 |
|  | X23 | 41,59 | 0,58 | 8,88 | 4,33 | 0,09 | 3,66 | 21,00 | 1,60 | 1,67 | 0,10 | 83,50 |
|  | X24 | 44,81 | 0,66 | 11,49 | 5,96 | 0,10 | 4,44 | 17,00 | 1,71 | 2,30 | 0,10 | 88,57 |
|  | X25 | 43,90 | 0,68 | 11,61 | 5,98 | 0,10 | 4,52 | 17,70 | 1,57 | 2,35 | 0,11 | 88,52 |
|  | X26 | 44,40 | 0,67 | 11,63 | 5,72 | 0,10 | 4,49 | 17,31 | 1,68 | 2,35 | 0,10 | 88,45 |
|  | X27 | 43,57 | 0,66 | 11,47 | 6,03 | 0,10 | 5,03 | 16,22 | 1,73 | 2,34 | 0,11 | 87,26 |
|  | X28 | 46,11 | 0,68 | 11,93 | 6,12 | 0,10 | 4,96 | 15,64 | 1,57 | 2,38 | 0,11 | 89,60 |
|  | X29 | 42,98 | 0,65 | 11,11 | 5,90 | 0,10 | 4,70 | 18,26 | 1,54 | 2,29 | 0,11 | 87,64 |
|  | X30 | 36,96 | 0,58 | 9,18 | 5,10 | 0,12 | 3,83 | 24,60 | 1,21 | 2,01 | 0,10 | 83,69 |
|  | X31 | 43,32 | 0,71 | 12,21 | 6,49 | 0,13 | 4,51 | 17,12 | 1,49 | 2,68 | 0,11 | 88,77 |
|  | X32 | 45,26 | 0,68 | 12,13 | 6,57 | 0,11 | 4,77 | 16,44 | 1,43 | 2,44 | 0,11 | 89,93 |
|  | X33 | 45,41 | 0,69 | 12,32 | 6,71 | 0,11 | 5,03 | 15,68 | 1,65 | 2,53 | 0,10 | 90,23 |
|  | X34 | 42,16 | 0,66 | 11,29 | 6,15 | 0,11 | 4,76 | 18,60 | 1,60 | 2,35 | 0,10 | 87,78 |
|  | X35 | 43,10 | 0,66 | 11,52 | 6,31 | 0,13 | 4,37 | 19,18 | 1,31 | 2,38 | 0,10 | 89,05 |
|  | X36 | 43,92 | 0,70 | 12,64 | 6,99 | 0,13 | 4,87 | 17,58 | 1,43 | 2,66 | 0,10 | 91,02 |
|  | X37 | 41,77 | 0,64 | 10,59 | 5,92 | 0,11 | 4,20 | 20,86 | 1,36 | 2,20 | 0,10 | 87,75 |
|  | X38 | 46,28 | 0,72 | 12,59 | 6,35 | 0,11 | 4,63 | 15,92 | 1,30 | 2,50 | 0,10 | 90,50 |
|  | X39 | 45,38 | 0,69 | 12,04 | 6,53 | 0,11 | 4,56 | 16,84 | 1,40 | 2,43 | 0,11 | 90,09 |
|  | X40 | 43,62 | 0,65 | 10,72 | 5,95 | 0,10 | 4,44 | 18,95 | 1,53 | 2,15 | 0,12 | 88,23 |
|  | X41 | 46,12 | 0,71 | 12,55 | 6,56 | 0,09 | 4,66 | 15,20 | 1,48 | 2,55 | 0,11 | 90,03 |
|  | X42 | 44,86 | 0,72 | 13,01 | 7,06 | 0,12 | 4,75 | 16,84 | 1,28 | 2,75 | 0,10 | 91,49 |
|  | X43 | 45,38 | 0,73 | 13,04 | 6,85 | 0,12 | 4,74 | 16,56 | 1,32 | 2,74 | 0,11 | 91,59 |
|  | X44 | 42,31 | 0,69 | 11,79 | 6,78 | 0,12 | 4,44 | 19,59 | 1,01 | 2,55 | 0,11 | 89,39 |
|  | X45 | 42,31 | 0,69 | 11,79 | 6,78 | 0,12 | 4,44 | 19,59 | 1,01 | 2,55 | 0,11 | 89,39 |
|  | X46 | 38,96 | 0,60 | 10,47 | 6,58 | 0,12 | 5,42 | 22,20 | 1,14 | 2,17 | 0,12 | 87,78 |
|  | X47 | 40,40 | 0,63 | 10,51 | 5,80 | 0,10 | 4,08 | 21,84 | 1,39 | 2,21 | 0,11 | 87,07 |
|  | X48 | 41,50 | 0,66 | 11,26 | 6,22 | 0,11 | 4,26 | 21,32 | 1,28 | 2,40 | 0,10 | 89,11 |
|  | X49 | 40,72 | 0,64 | 10,91 | 6,10 | 0,12 | 4,32 | 21,03 | 1,45 | 2,31 | 0,11 | 87,70 |
|  | X50 | 41,20 | 0,65 | 10,88 | 5,92 | 0,11 | 4,04 | 21,13 | 1,00 | 2,38 | 0,11 | 87,42 |
|  | X51 | 43,33 | 0,68 | 12,13 | 7,14 | 0,11 | 5,33 | 18,43 | 0,97 | 2,57 | 0,11 | 90,79 |
|  | X53 | 43,31 | 0,67 | 11,83 | 6,92 | 0,12 | 4,57 | 18,96 | 1,26 | 2,50 | 0,11 | 90,25 |
|  | X71 | 3,06 | 0,07 | 0,50 | 5,40 | 0,16 | 5,04 | 42,48 | 0,62 | 0,15 | 0,17 | 57,65 |
| Koutala beach/Kefalonia | Κ0 | 45,56 | 0,72 | 12,78 | 6,92 | 0,12 | 4,66 | 16,93 | 1,29 | 2,70 | 0,10 | 91,77 |
|  | Κ1 | 37,42 | 0,60 | 9,75 | 5,71 | 0,13 | 3,96 | 24,25 | 1,18 | 2,12 | 0,12 | 85,24 |
|  | Κ3 | 42,64 | 0,66 | 11,53 | 6,45 | 0,11 | 4,99 | 19,14 | 1,35 | 2,40 | 0,11 | 89,36 |
|  | Κ4 | 41,45 | 0,65 | 10,97 | 6,16 | 0,12 | 4,34 | 21,51 | 1,21 | 2,39 | 0,11 | 88,90 |
|  | Κ5 | 42,89 | 0,68 | 12,21 | 6,69 | 0,11 | 4,70 | 19,84 | 1,41 | 2,67 | 0,12 | 91,31 |
|  | Κ6 | 43,15 | 0,68 | 11,74 | 6,63 | 0,11 | 4,39 | 20,25 | 1,14 | 2,49 | 0,11 | 90,68 |
|  | Κ8 | 46,33 | 0,75 | 13,70 | 7,04 | 0,09 | 4,87 | 15,56 | 1,42 | 2,93 | 0,10 | 92,79 |
| Matzavinata/Kefalonia | ΜΑ1 | 41,91 | 0,66 | 11,07 | 6,14 | 0,12 | 4,23 | 21,41 | 1,01 | 2,35 | 0,10 | 88,99 |
|  | ΜΑ2 | 42,85 | 0,67 | 11,50 | 6,41 | 0,13 | 4,30 | 19,37 | 1,35 | 2,37 | 0,10 | 89,05 |
|  | ΜΑ3 | 41,54 | 0,66 | 11,15 | 6,11 | 0,13 | 4,18 | 20,46 | 1,25 | 2,37 | 0,10 | 87,94 |
|  | ΜΑ4 | 44,14 | 0,71 | 12,42 | 6,84 | 0,14 | 4,55 | 17,46 | 1,39 | 2,59 | 0,10 | 90,33 |
|  | ΜΑ5 | 44,83 | 0,71 | 12,65 | 6,80 | 0,13 | 4,70 | 17,70 | 0,99 | 2,65 | 0,11 | 91,27 |
|  | ΜΑ6 | 42,74 | 0,68 | 11,89 | 6,73 | 0,13 | 4,57 | 19,81 | 0,99 | 2,58 | 0,10 | 90,22 |
|  | ΜΑ7 | 38,70 | 0,60 | 9,65 | 5,81 | 0,12 | 4,07 | 24,51 | 0,86 | 2,13 | 0,10 | 86,55 |
|  | ΜΑ8 | 42,86 | 0,68 | 11,61 | 6,92 | 0,13 | 4,30 | 18,51 | 1,15 | 2,43 | 0,11 | 88,71 |
|  | ΜΑ9 | 45,23 | 0,73 | 13,00 | 6,89 | 0,13 | 4,93 | 16,79 | 1,03 | 2,66 | 0,11 | 91,50 |
|  | ΜΑ10 | 43,81 | 0,72 | 12,49 | 6,62 | 0,12 | 4,72 | 17,42 | 1,26 | 2,62 | 0,11 | 89,88 |
|  | ΜΑ11 | 42,78 | 0,69 | 11,93 | 6,68 | 0,13 | 4,56 | 19,08 | 1,17 | 2,62 | 0,10 | 89,73 |
|  | ΜΑ12 | 36,42 | 0,59 | 9,19 | 5,52 | 0,12 | 3,87 | 25,89 | 0,93 | 2,06 | 0,11 | 84,70 |
|  | ΜΑ13 | 37,71 | 0,60 | 9,69 | 5,37 | 0,10 | 3,75 | 25,18 | 1,04 | 2,08 | 0,10 | 85,61 |
|  | ΜΑ14 | 35,44 | 0,56 | 8,97 | 5,58 | 0,10 | 3,56 | 27,16 | 1,07 | 1,93 | 0,11 | 84,48 |
|  | ΜΑ15 | 47,97 | 0,75 | 14,02 | 7,45 | 0,11 | 5,49 | 13,56 | 0,92 | 2,88 | 0,11 | 93,25 |
| Chavdata/Kefalonia | CH1 | 39,92 | 0,62 | 10,75 | 6,28 | 0,14 | 4,18 | 24,00 | 1,17 | 2,38 | 0,12 | 89,55 |
|  | CH2 | 46,53 | 0,75 | 13,35 | 7,40 | 0,13 | 4,99 | 15,61 | 1,24 | 2,80 | 0,11 | 92,88 |
|  | CH3 | 47,37 | 0,79 | 14,27 | 7,78 | 0,12 | 5,38 | 13,87 | 1,20 | 2,97 | 0,12 | 93,86 |
|  | CH4 | 40,59 | 0,64 | 10,88 | 6,55 | 0,14 | 4,40 | 23,00 | 0,89 | 2,40 | 0,11 | 89,60 |
|  | CH5 | 36,91 | 0,59 | 9,55 | 5,73 | 0,11 | 3,82 | 26,78 | 1,02 | 2,05 | 0,10 | 86,67 |
|  | CH6 | 38,41 | 0,61 | 10,17 | 6,06 | 0,12 | 3,83 | 25,64 | 0,83 | 2,26 | 0,10 | 88,02 |
|  | CH7 | 39,35 | 0,64 | 10,83 | 6,37 | 0,11 | 4,16 | 23,77 | 0,87 | 2,43 | 0,11 | 88,63 |
|  | CH8 | 42,55 | 0,68 | 11,93 | 6,86 | 0,12 | 4,57 | 21,20 | 0,89 | 2,64 | 0,11 | 91,54 |
|  | CH9 | 44,93 | 0,73 | 13,07 | 8,12 | 0,14 | 4,59 | 15,89 | 0,92 | 2,82 | 0,10 | 91,31 |
|  | CH10 | 46,26 | 0,74 | 13,03 | 6,93 | 0,11 | 4,50 | 15,89 | 0,94 | 2,78 | 0,09 | 91,27 |
|  | CH12 | 46,28 | 0,72 | 13,04 | 7,33 | 0,11 | 4,89 | 16,43 | 0,96 | 2,80 | 0,11 | 92,66 |
|  | CH14 | 44,52 | 0,73 | 12,94 | 6,91 | 0,10 | 4,89 | 18,24 | 0,98 | 2,78 | 0,11 | 92,20 |
|  | CH15 | 42,70 | 0,72 | 12,82 | 6,93 | 0,11 | 4,90 | 19,16 | 1,20 | 2,74 | 0,10 | 91,38 |
|  | CH17 | 41,96 | 0,67 | 11,73 | 6,90 | 0,12 | 4,43 | 21,14 | 0,96 | 2,62 | 0,11 | 90,64 |
|  | CH18 | 41,93 | 0,65 | 11,17 | 6,58 | 0,12 | 4,22 | 22,23 | 1,06 | 2,48 | 0,11 | 90,54 |
| Arillas beach/Corfu | Β2 | 34,67 | 0,60 | 9,96 | 6,16 | 0,15 | 4,90 | 26,99 | 0,76 | 2,24 | 0,11 | 86,53 |
|  | Β3 | 38,06 | 0,63 | 10,88 | 6,58 | 0,12 | 4,91 | 23,82 | 1,04 | 2,45 | 0,08 | 88,55 |
|  | Β4 | 38,54 | 0,64 | 10,98 | 7,01 | 0,14 | 5,26 | 22,47 | 0,66 | 2,46 | 0,09 | 88,24 |
|  | Β5 | 35,54 | 0,61 | 10,19 | 6,45 | 0,16 | 4,73 | 26,35 | 0,83 | 2,28 | 0,10 | 87,22 |
|  | Β6 | 39,84 | 0,65 | 11,31 | 6,94 | 0,13 | 5,29 | 21,73 | 0,92 | 2,47 | 0,09 | 89,36 |
|  | Β7 | 33,92 | 0,58 | 9,80 | 6,16 | 0,14 | 4,67 | 27,28 | 1,23 | 2,22 | 0,11 | 86,12 |
|  | Β8 | 32,80 | 0,57 | 9,58 | 6,22 | 0,18 | 4,43 | 29,25 | 1,09 | 2,19 | 0,13 | 86,42 |
|  | Β9 | 35,46 | 0,61 | 10,38 | 6,76 | 0,15 | 4,65 | 25,99 | 1,10 | 2,32 | 0,12 | 87,52 |
|  | Β10 | 38,62 | 0,64 | 10,88 | 6,81 | 0,13 | 5,12 | 21,65 | 1,25 | 2,41 | 0,09 | 87,59 |
|  | Β11 | 35,58 | 0,61 | 10,28 | 6,38 | 0,12 | 4,73 | 25,01 | 1,13 | 2,34 | 0,10 | 86,27 |
|  | Β12 | 36,94 | 0,59 | 10,40 | 6,56 | 0,14 | 5,54 | 23,68 | 1,19 | 2,28 | 0,09 | 87,41 |
|  | Β15 | 36,80 | 0,62 | 10,36 | 6,27 | 0,14 | 4,93 | 24,68 | 1,04 | 2,33 | 0,10 | 87,26 |
|  | Β17 | 37,68 | 0,61 | 10,41 | 6,59 | 0,12 | 5,25 | 23,83 | 1,08 | 2,31 | 0,08 | 87,96 |
|  | Β19 | 40,08 | 0,64 | 11,19 | 6,86 | 0,13 | 5,57 | 21,45 | 1,14 | 2,44 | 0,09 | 89,59 |
|  | Β21 | 37,88 | 0,61 | 10,16 | 6,63 | 0,17 | 5,70 | 23,51 | 0,58 | 2,20 | 0,11 | 87,55 |
|  | Β22 | 41,15 | 0,64 | 11,42 | 6,73 | 0,11 | 7,06 | 19,06 | 0,66 | 2,50 | 0,08 | 89,42 |
|  | Β31 | 33,49 | 0,55 | 9,54 | 5,89 | 0,13 | 4,05 | 30,25 | 0,48 | 2,09 | 0,10 | 86,58 |
|  | Β33 | 36,23 | 0,59 | 9,62 | 6,29 | 0,13 | 3,88 | 26,76 | 0,59 | 2,02 | 0,10 | 86,21 |
|  | Β39 | 35,19 | 0,59 | 10,31 | 7,05 | 0,12 | 4,74 | 25,93 | 0,50 | 2,19 | 0,09 | 86,70 |
|  | Β41 | 40,56 | 0,62 | 10,49 | 6,30 | 0,14 | 6,46 | 20,27 | 0,80 | 2,07 | 0,11 | 87,81 |
| Agios Stefanos beach/Corfu | Α0 | 40,43 | 0,62 | 10,47 | 6,84 | 0,11 | 5,42 | 23,62 | 0,59 | 2,30 | 0,11 | 90,51 |
|  | Α1 | 37,50 | 0,58 | 9,29 | 6,28 | 0,12 | 5,02 | 26,63 | 0,52 | 2,06 | 0,12 | 88,11 |
|  | Α2΄ | 40,93 | 0,63 | 10,86 | 7,25 | 0,13 | 6,17 | 22,43 | 0,58 | 2,33 | 0,12 | 91,41 |
|  | Α4 | 44,32 | 0,66 | 11,57 | 7,35 | 0,12 | 6,81 | 17,96 | 0,69 | 2,52 | 0,10 | 92,09 |
|  | Α5 | 40,46 | 0,61 | 10,42 | 6,68 | 0,12 | 5,82 | 22,67 | 0,57 | 2,34 | 0,12 | 89,81 |
|  | Α6 | 36,57 | 0,61 | 9,83 | 7,40 | 0,15 | 5,07 | 25,89 | 0,43 | 2,11 | 0,14 | 88,20 |
|  | Α7 | 43,52 | 0,66 | 11,89 | 7,45 | 0,13 | 6,11 | 21,23 | 0,52 | 2,52 | 0,11 | 94,14 |
|  | Α8 | 45,15 | 0,69 | 12,26 | 7,86 | 0,13 | 6,49 | 16,76 | 0,57 | 2,58 | 0,11 | 92,59 |
|  | Α9 | 44,43 | 0,66 | 11,83 | 7,64 | 0,17 | 6,48 | 16,97 | 0,86 | 2,62 | 0,10 | 91,75 |
|  | Α10 | 43,98 | 0,65 | 11,40 | 7,26 | 0,11 | 6,40 | 18,51 | 0,58 | 2,47 | 0,10 | 91,46 |
|  | Α11 | 41,54 | 0,65 | 11,16 | 7,12 | 0,12 | 5,85 | 21,20 | 0,54 | 2,41 | 0,10 | 90,68 |
|  | Α12 | 42,13 | 0,65 | 11,31 | 7,44 | 0,13 | 6,11 | 19,82 | 0,54 | 2,40 | 0,10 | 90,63 |
|  | Α13 | 41,64 | 0,65 | 11,20 | 7,82 | 0,14 | 6,04 | 20,12 | 0,55 | 2,43 | 0,11 | 90,68 |
|  | Α14 | 40,20 | 0,61 | 10,01 | 6,62 | 0,12 | 5,45 | 22,04 | 0,61 | 2,21 | 0,11 | 87,98 |
|  | Α15 | 40,27 | 0,62 | 10,51 | 6,99 | 0,12 | 5,71 | 22,29 | 0,50 | 2,37 | 0,11 | 89,48 |
|  | Α16 | 42,19 | 0,64 | 11,20 | 6,85 | 0,11 | 5,85 | 19,74 | 0,81 | 2,46 | 0,10 | 89,94 |
|  | Α17 | 39,52 | 0,61 | 10,27 | 6,68 | 0,11 | 5,54 | 22,46 | 0,86 | 2,30 | 0,11 | 88,45 |
|  | Α18 | 36,25 | 0,58 | 9,45 | 6,56 | 0,11 | 4,99 | 26,39 | 0,43 | 2,19 | 0,11 | 87,06 |
|  | Α19 | 35,64 | 0,58 | 9,35 | 6,51 | 0,11 | 4,70 | 26,22 | 0,86 | 2,12 | 0,12 | 86,21 |
|  | Α20 | 39,79 | 0,64 | 10,52 | 6,96 | 0,11 | 5,23 | 22,61 | 0,49 | 2,28 | 0,09 | 88,73 |

Table S3: Mineralogical com-position.

| Location | Samples | Quartz | Calcite | Plagioclase | Illite | Chlorite | Kaolinite | Smectite | Dolomite | Total (%) | Clay minerals |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Xi beach/Kefalonia | X10 | 39 | 34 | 9 | 6 | 2 | 5 | 2 | 3 | 100 | 9 |
|  | X11 | 37 | 41 | 8 | 4 | 3 | 4 | 1 | 2 | 100 | 8 |
|  | X12 | 39 | 31 | 7 | 8 | 4 | 4 | 2 | 5 | 100 | 10 |
|  | X13 | 39 | 32 | 9 | 5 | 5 | 4 | 2 | 4 | 100 | 11 |
|  | X14 | 38 | 31 | 10 | 8 | 5 | 4 | 2 | 2 | 100 | 11 |
|  | X15 | 40 | 32 | 10 | 6 | 3 | 3 | 3 | 3 | 100 | 9 |
|  | X16 | 41 | 28 | 11 | 5 | 5 | 6 | 2 | 2 | 100 | 13 |
|  | X17 | 41 | 30 | 10 | 7 | 4 | 4 | 1 | 3 | 100 | 9 |
|  | X18 | 40 | 29 | 10 | 6 | 5 | 5 | 2 | 3 | 100 | 12 |
|  | X19 | 42 | 27 | 11 | 6 | 5 | 5 | 2 | 2 | 100 | 12 |
|  | X21 | 40 | 37 | 8 | 4 | 2 | 5 | 2 | 2 | 100 | 9 |
|  | X22 | 41 | 30 | 9 | 5 | 5 | 5 | 2 | 3 | 100 | 12 |
|  | X23 | 42 | 30 | 12 | 4 | 3 | 2 | 3 | 4 | 100 | 8 |
|  | X24 | 38 | 33 | 11 | 6 | 3 | 4 | 2 | 3 | 100 | 9 |
|  | X25 | 41 | 30 | 12 | 4 | 3 | 3 | 3 | 4 | 100 | 9 |
|  | X26 | 37 | 34 | 11 | 7 | 4 | 4 | 1 | 2 | 100 | 9 |
|  | X27 | 42 | 28 | 11 | 4 | 4 | 4 | 1 | 6 | 100 | 9 |
|  | X28 | 41 | 31 | 9 | 6 | 5 | 3 | 1 | 4 | 100 | 9 |
|  | X29 | 41 | 29 | 12 | 5 | 4 | 4 | 2 | 3 | 100 | 10 |
|  | X30 | 39 | 35 | 11 | 5 | 3 | 3 | 2 | 2 | 100 | 8 |
|  | X31 | 36 | 30 | 12 | 9 | 5 | 5 | 1 | 2 | 100 | 11 |
|  | X32 | 41 | 31 | 12 | 5 | 4 | 4 | 1 | 2 | 100 | 9 |
|  | X33 | 43 | 28 | 10 | 5 | 5 | 4 | 1 | 4 | 100 | 10 |
|  | X34 | 40 | 31 | 13 | 4 | 3 | 3 | 1 | 5 | 100 | 7 |
|  | X35 | 41 | 32 | 10 | 5 | 4 | 4 | 1 | 3 | 100 | 9 |
|  | X36 | 37 | 31 | 11 | 5 | 6 | 4 | 1 | 5 | 100 | 11 |
|  | X37 | 37 | 33 | 12 | 7 | 4 | 3 | 1 | 3 | 100 | 8 |
|  | X38 | 36 | 27 | 16 | 8 | 4 | 4 | 2 | 3 | 100 | 10 |
|  | X39 | 41 | 27 | 15 | 6 | 3 | 3 | 1 | 4 | 100 | 7 |
|  | X40 | 35 | 28 | 16 | 7 | 5 | 6 | 1 | 2 | 100 | 12 |
|  | X41 | 40 | 27 | 15 | 6 | 3 | 4 | 2 | 3 | 100 | 9 |
|  | X42 | 38 | 35 | 12 | 4 | 4 | 3 | 2 | 2 | 100 | 9 |
|  | X43 | 37 | 31 | 10 | 8 | 5 | 4 | 2 | 3 | 100 | 11 |
|  | X44 | 38 | 34 | 9 | 7 | 4 | 3 | 2 | 3 | 100 | 9 |
|  | X45 | 38 | 35 | 10 | 6 | 4 | 3 | 2 | 2 | 100 | 9 |
|  | X46 | 36 | 33 | 10 | 3 | 3 | 2 | 1 | 12 | 100 | 6 |
|  | X47 | 42 | 36 | 10 | 5 | 2 | 2 | 1 | 2 | 100 | 5 |
|  | X48 | 43 | 33 | 10 | 5 | 4 | 3 | 1 | 1 | 100 | 8 |
|  | X49 | 44 | 32 | 10 | 5 | 4 | 3 | 1 | 1 | 100 | 8 |
|  | X50 | 39 | 32 | 11 | 5 | 5 | 5 | 1 | 2 | 100 | 11 |
|  | X51 | 37 | 31 | 12 | 5 | 3 | 3 | 1 | 8 | 100 | 7 |
|  | X53 | 40 | 35 | 12 | 5 | 3 | 2 | 1 | 2 | 100 | 6 |
| Koutala beach/Kefalonia | Κ0 | 33 | 33 | 14 | 5 | 7 | 6 | 1 | 1 | 100 | 14 |
|  | Κ1 | 31 | 37 | 10 | 7 | 5 | 4 | 4 | 2 | 100 | 13 |
|  | Κ3 | 35 | 28 | 13 | 10 | 6 | 4 | 1 | 3 | 100 | 11 |
|  | Κ4 | 30 | 36 | 14 | 9 | 4 | 4 | 3 | 1 | 100 | 11 |
|  | Κ5 | 39 | 32 | 7 | 5 | 8 | 6 | 1 | 2 | 100 | 15 |
|  | Κ6 | 33 | 33 | 8 | 12 | 7 | 5 | 1 | 1 | 100 | 13 |
|  | Κ8 | 36 | 31 | 10 | 7 | 7 | 6 | 1 | 2 | 100 | 14 |
| Matzavinata/Kefalonia | MA1 | 36 | 34 | 10 | 8 | 5 | 4 | 1 | 2 | 100 | 10 |
|  | MA2 | 39 | 33 | 11 | 5 | 4 | 4 | 1 | 3 | 100 | 9 |
|  | MA3 | 38 | 36 | 10 | 6 | 3 | 4 | 1 | 2 | 100 | 8 |
|  | MA4 | 45 | 30 | 10 | 4 | 4 | 4 | 1 | 2 | 100 | 9 |
|  | MA5 | 40 | 30 | 11 | 5 | 5 | 4 | 2 | 3 | 100 | 11 |
|  | MA6 | 38 | 35 | 13 | 5 | 3 | 3 | 1 | 2 | 100 | 7 |
|  | MA7 | 37 | 38 | 12 | 4 | 3 | 3 | 1 | 2 | 100 | 7 |
|  | MA8 | 42 | 31 | 10 | 5 | 4 | 4 | 1 | 3 | 100 | 9 |
|  | MA9 | 40 | 30 | 13 | 2 | 5 | 6 | 2 | 2 | 100 | 13 |
|  | MA10 | 42 | 31 | 9 | 7 | 4 | 4 | 1 | 2 | 100 | 9 |
|  | MA11 | 35 | 36 | 11 | 4 | 4 | 4 | 4 | 2 | 100 | 12 |
|  | MA12 | 41 | 39 | 10 | 3 | 2 | 2 | 2 | 1 | 100 | 6 |
|  | MA13 | 43 | 39 | 7 | 4 | 2 | 2 | 2 | 1 | 100 | 6 |
|  | MA14 | 42 | 38 | 8 | 3 | 2 | 3 | 2 | 2 | 100 | 7 |
|  | MA15 | 42 | 24 | 15 | 4 | 4 | 5 | 1 | 5 | 100 | 10 |
| Chavdata/Kefalonia | CH1 | 36 | 38 | 13 | 6 | 2 | 2 | 1 | 2 | 100 | 11 |
|  | CH2 | 34 | 31 | 15 | 6 | 4 | 5 | 2 | 3 | 100 | 17 |
|  | CH3 | 32 | 27 | 16 | 7 | 8 | 6 | 1 | 3 | 100 | 22 |
|  | CH4 | 32 | 40 | 11 | 5 | 4 | 4 | 2 | 2 | 100 | 15 |
|  | CH5 | 30 | 37 | 15 | 4 | 5 | 4 | 2 | 3 | 100 | 15 |
|  | CH6 | 34 | 40 | 8 | 5 | 4 | 5 | 1 | 3 | 100 | 15 |
|  | CH7 | 32 | 42 | 9 | 4 | 4 | 4 | 2 | 3 | 100 | 14 |
|  | CH8 | 40 | 39 | 6 | 5 | 3 | 3 | 1 | 3 | 100 | 12 |
|  | CH9 | 45 | 32 | 8 | 4 | 3 | 3 | 2 | 3 | 100 | 12 |
|  | CH10 | 45 | 34 | 10 | 3 | 2 | 2 | 2 | 2 | 100 | 9 |
|  | CH12 | 45 | 28 | 8 | 6 | 5 | 3 | 1 | 4 | 100 | 15 |
|  | CH14 | 37 | 34 | 8 | 7 | 4 | 4 | 1 | 5 | 100 | 16 |
|  | CH15 | 35 | 30 | 8 | 8 | 5 | 7 | 2 | 5 | 100 | 22 |
|  | CH17 | 39 | 35 | 8 | 6 | 4 | 3 | 2 | 3 | 100 | 15 |
|  | CH18 | 39 | 39 | 7 | 6 | 2 | 3 | 1 | 3 | 100 | 12 |
| Arillas beach/Corfu | B2 | 25 | 39 | 9 | 8 | 9 | 2 | 2 | 6 | 100 | 13 |
|  | B3 | 25 | 37 | 10 | 7 | 12 | 4 | 2 | 3 | 100 | 18 |
|  | B4 | 23 | 35 | 9 | 8 | 12 | 5 | 4 | 4 | 100 | 21 |
|  | B5 | 26 | 38 | 8 | 7 | 13 | 3 | 2 | 3 | 100 | 18 |
|  | B6 | 26 | 36 | 11 | 7 | 12 | 5 | 1 | 2 | 100 | 18 |
|  | B7 | 26 | 39 | 9 | 6 | 11 | 2 | 4 | 3 | 100 | 17 |
|  | B8 | 27 | 40 | 6 | 9 | 10 | 3 | 2 | 3 | 100 | 15 |
|  | B9 | 22 | 37 | 8 | 9 | 11 | 5 | 4 | 4 | 100 | 20 |
|  | B10 | 25 | 34 | 9 | 8 | 14 | 5 | 2 | 3 | 100 | 21 |
|  | B11 | 26 | 39 | 7 | 9 | 11 | 2 | 1 | 5 | 100 | 14 |
|  | B12 | 28 | 28 | 6 | 12 | 12 | 5 | 3 | 6 | 100 | 20 |
|  | B15 | 22 | 31 | 6 | 6 | 10 | 4 | 2 | 19 | 100 | 16 |
|  | B17 | 29 | 33 | 9 | 9 | 9 | 4 | 2 | 5 | 100 | 15 |
|  | B19 | 28 | 29 | 12 | 9 | 11 | 5 | 2 | 4 | 100 | 18 |
|  | B21 | 26 | 38 | 6 | 7 | 13 | 2 | 4 | 4 | 100 | 19 |
|  | B22 | 31 | 31 | 6 | 7 | 11 | 3 | 4 | 7 | 100 | 18 |
|  | B31 | 23 | 49 | 7 | 6 | 8 | 3 | 3 | 1 | 100 | 14 |
|  | B33 | 29 | 40 | 8 | 6 | 7 | 3 | 6 | 1 | 100 | 16 |
|  | B39 | 30 | 41 | 6 | 3 | 8 | 7 | 3 | 2 | 100 | 18 |
|  | B41 | 37 | 25 | 14 | 6 | 8 | 4 | 2 | 4 | 100 | 14 |
| Agios Stefanos beach/Corfu | A0 | 30 | 36 | 10 | 4 | 11 | 4 | 2 | 3 | 100 | 21 |
|  | A1 | 27 | 41 | 7 | 6 | 10 | 4 | 2 | 3 | 100 | 22 |
|  | A2' | 28 | 39 | 8 | 7 | 9 | 3 | 4 | 2 | 100 | 23 |
|  | A4 | 29 | 33 | 7 | 8 | 12 | 5 | 3 | 3 | 100 | 28 |
|  | A5 | 28 | 31 | 11 | 7 | 11 | 6 | 3 | 3 | 100 | 27 |
|  | A6 | 29 | 39 | 8 | 7 | 10 | 4 | 2 | 1 | 100 | 23 |
|  | A7 | 31 | 43 | 6 | 3 | 9 | 2 | 4 | 2 | 100 | 18 |
|  | A8 | 27 | 36 | 6 | 9 | 11 | 6 | 4 | 1 | 100 | 30 |
|  | A9 | 30 | 31 | 9 | 6 | 11 | 5 | 5 | 3 | 100 | 27 |
|  | A10 | 29 | 31 | 8 | 8 | 11 | 7 | 4 | 2 | 100 | 30 |
|  | A11 | 27 | 38 | 7 | 7 | 10 | 5 | 4 | 2 | 100 | 26 |
|  | A12 | 28 | 32 | 8 | 7 | 11 | 7 | 3 | 4 | 100 | 28 |
|  | A13 | 28 | 33 | 6 | 6 | 11 | 7 | 5 | 4 | 100 | 29 |
|  | A14 | 28 | 32 | 12 | 7 | 9 | 6 | 3 | 3 | 100 | 25 |
|  | A15 | 26 | 38 | 7 | 10 | 8 | 5 | 3 | 3 | 100 | 26 |
|  | A16 | 29 | 30 | 8 | 10 | 11 | 8 | 2 | 2 | 100 | 31 |
|  | A17 | 28 | 36 | 9 | 9 | 8 | 6 | 2 | 2 | 100 | 25 |
|  | A18 | 28 | 35 | 8 | 6 | 9 | 7 | 4 | 3 | 100 | 26 |
|  | A19 | 27 | 36 | 8 | 6 | 9 | 7 | 4 | 3 | 100 | 26 |
|  | A20 | 29 | 33 | 8 | 9 | 9 | 5 | 4 | 3 | 100 | 27 |

Table S4: pH determination results.

| Location | Samples | pH | T°C | Determination by Soil Survey Staff 2017 |
| --- | --- | --- | --- | --- |
| Xi beach/Kefalonia | X10 | 8.2 | 26 | Moderately alkaline |  |
|  | X11 | 8.9 | 24.3 | Strongly alkaline |  |
|  | X12 | 8.6 | 25.3 | Strongly alkaline |  |
|  | X13 | 8.6 | 25 | Strongly alkaline |  |
|  | X14 | 8.4 | 24.2 | Moderately alkaline |  |
|  | X15 | 8.1 | 24.7 | Moderately alkaline |  |
|  | X16 | 8.2 | 24.5 | Moderately alkaline |  |
|  | X17 | 8.4 | 24.5 | Moderately alkaline |  |
|  | X18 | 8.7 | 25.4 | Strongly alkaline |  |
|  | X19 | 8.1 | 24.7 | Moderately alkaline |  |
|  | X21 | 8 | 24.3 | Moderately alkaline |  |
|  | X22 | 8.4 | 25.8 | Moderately alkaline |  |
|  | X23 | 8.5 | 25 | Moderately alkaline |  |
|  | X24 | 8.6 | 25.1 | Strongly alkaline |  |
|  | X25 | 8.7 | 25 | Strongly alkaline |  |
|  | X26 | 8.6 | 25.1 | Strongly alkaline |  |
|  | X27 | 8.5 | 24.7 | Strongly alkaline |  |
|  | X28 | 8.2 | 24.6 | Moderately alkaline |  |
|  | X29 | 7.8 | 25.1 | Slightly alkaline |  |
|  | X30 | 8.7 | 25.1 | Strongly alkaline |  |
|  | X31 | 8.8 | 25 | Strongly alkaline |  |
|  | X32 | 8 | 24.2 | Moderately alkaline |  |
|  | X33 | 8.2 | 24.3 | Moderately alkaline |  |
|  | X34 | 8.6 | 24.4 | Strongly alkaline |  |
|  | X35 | 8.6 | 24.9 | Strongly alkaline |  |
|  | X36 | 8.5 | 25.2 | Moderately alkaline |  |
|  | X37 | 8.3 | 25.2 | Moderately alkaline |  |
|  | X38 | 8.7 | 25.4 | Strongly alkaline |  |
|  | X39 | 8.4 | 24.5 | Moderately alkaline |  |
|  | X40 | 8.2 | 25.3 | Moderately alkaline |  |
|  | X41 | 8.1 | 25.3 | Strongly alkaline |  |
|  | X42 | 8.8 | 25.1 | Strongly alkaline |  |
|  | X43 | 8.7 | 25.1 | Strongly alkaline |  |
|  | X44 | 8.8 | 25.1 | Strongly alkaline |  |
|  | X45 | 9.6 | 23.9 | Very Strongly alkaline |  |
|  | X46 | 8.2 | 25.5 | Moderately alkaline |  |
|  | X47 | 8.6 | 23.9 | Strongly alkaline |  |
|  | X48 | 8.7 | 25 | Strongly alkaline |  |
|  | X49 | 8.5 | 24.2 | Moderately alkaline |  |
|  | X50 | 8.4 | 24.9 | Moderately alkaline |  |
|  | X51 | 8.1 | 25.3 | Moderately alkaline |  |
|  | X53 | 8.5 | 24.9 | Strongly alkaline |  |
| Koutala beach/Kefalonia | K0 | 8.7 | 25.5 | Strongly alkaline |  |
|  | K1 | 9.1 | 26 | Very Strongly alkaline |  |
|  | K2 | 8.4 | 25.4 | Moderately alkaline |  |
|  | K3 | 8.3 | 25 | Moderately alkaline |  |
|  | K4 | 9 | 25 | Moderately alkaline |  |
|  | K5 | 9 | 25.4 | Moderately alkaline |  |
|  | K6 | 8.5 | 25.8 | Moderately alkaline |  |
|  | K8 | 9.3 | 25 | Very Strongly alkaline |  |
| Matzavinata/Kefalonia | MA1 | 8.9 | 26.1 | Strongly alkaline |  |
|  | MA2 | 9 | 26 | Strongly alkaline |  |
|  | MA3 | 9.6 | 25.3 | Very Strongly alkaline |  |
|  | MA4 | 9.1 | 25.8 | Strongly alkaline |  |
|  | MA5 | 9.1 | 25.8 | Strongly alkaline |  |
|  | MA6 | 9.1 | 25.8 | Strongly alkaline |  |
|  | MA7 | 8.8 | 25.7 | Strongly alkaline |  |
|  | MA8 | 9.2 | 25.6 | Very Strongly alkaline |  |
|  | MA9 | 9.2 | 25.7 | Very Strongly alkaline |  |
|  | MA10 | 8.9 | 25.5 | Strongly alkaline |  |
|  | MA11 | 9.1 | 25.5 | Strongly alkaline |  |
|  | MA12 | 8.9 | 25.3 | Strongly alkaline |  |
|  | MA13 | 9 | 25.2 | Strongly alkaline |  |
|  | MA14 | 9.2 | 24.7 | Very Strongly alkaline |  |
|  | MA15 | 8.4 | 24.6 | Moderately alkaline |  |
| Chavdata/Kefalonia | CH1 | 9.1 | 25 | Very Strongly alkaline |  |
|  | CH2 | 9.2 | 25.8 | Very Strongly alkaline |  |
|  | CH3 | 8.9 | 24.6 | Strongly alkaline |  |
|  | CH4 | 9.3 | 24.6 | Very Strongly alkaline |  |
|  | CH5 | 9.2 | 25.1 | Very Strongly alkaline |  |
|  | CH6 | 8.9 | 24.7 | Strongly alkaline |  |
|  | CH7 | 8.9 | 25 | Strongly alkaline |  |
|  | CH8 | 9.2 | 24.4 | Very Strongly alkaline |  |
|  | CH9 | 9.2 | 25.3 | Very Strongly alkaline |  |
|  | CH10 | 8.9 | 24.5 | Strongly alkaline |  |
|  | CH11 | 9.1 | 25.3 | Strongly alkaline |  |
|  | CH12 | 9.1 | 25.3 | Very Strongly alkaline |  |
|  | CH13 | 9.1 | 25.3 | Strongly alkaline |  |
|  | CH14 | 9.2 | 24.6 | Very Strongly alkaline |  |
|  | CH15 | 9.6 | 24.7 | Very Strongly alkaline |  |
|  | CH16 | 9.5 | 25.1 | Very Strongly alkaline |  |
|  | CH17 | 9.4 | 24.8 | Very Strongly alkaline |  |
|  | CH18 | 9.2 | 24.9 | Very Strongly alkaline |  |
| Arillas beach/Corfu | B2 | 8.5 | 24.6 | Strongly alkaline |  |
|  | B3 | 9 | 24 | Strongly alkaline |  |
|  | B4 | 9.1 | 23.9 | Strongly alkaline |  |
|  | B5 | 8.4 | 24.6 | Moderately alkaline |  |
|  | B6 | 9.3 | 24 | Strongly alkaline |  |
|  | B7 | 9 | 23.8 | Strongly alkaline |  |
|  | B8 | 8.9 | 23.2 | Strongly alkaline |  |
|  | B9 | 9.2 | 23.8 | Strongly alkaline |  |
|  | B10 | 8.8 | 23.6 | Strongly alkaline |  |
|  | B11 | 8.8 | 23.5 | Strongly alkaline |  |
|  | B12 | 8.6 | 23.1 | Strongly alkaline |  |
|  | B15 | 9.6 | 2523 | Strongly alkaline |  |
|  | B17 | 9.1 | 23.5 | Strongly alkaline |  |
|  | B19 | 9.6 | 23.4 | Strongly alkaline |  |
|  | B21 | 8.9 | 23.4 | Strongly alkaline |  |
|  | B22 | 8.4 | 23.2 | Moderately alkaline |  |
|  | B31 | 8.5 | 23.2 | Moderately alkaline |  |
|  | B33 | 9 | 23.1 | Strongly alkaline |  |
|  | B39 | 8.9 | 22.6 | Strongly alkaline |  |
|  | B41 | 8.2 | 23 | Moderately alkaline |  |
| Agios Stefanos beach/Corfu | A0 | 8.3 | 24.5 | Moderately alkaline |  |
|  | A1 | 8.1 | 25.1 | Moderately alkaline |  |
|  | A4 | 8.2 | 23 | Moderately alkaline |  |
|  | A5 | 8.2 | 23.2 | Moderately alkaline |  |
|  | A6 | 8.3 | 24.3 | Moderately alkaline |  |
|  | A7 | 8.3 | 23.6 | Moderately alkaline |  |
|  | A8 | 8.5 | 24.5 | Strongly alkaline |  |
|  | A9 | 8.1 | 24.3 | Moderately alkaline |  |
|  | A10 | 8.2 | 23.9 | Moderately alkaline |  |
|  | A11 | 8.5 | 23.8 | Strongly alkaline |  |
|  | A12 | 8.4 | 23.8 | Moderately alkaline |  |
|  | A13 | 8.4 | 23.6 | Moderately alkaline |  |
|  | A14 | 8.3 | 23.6 | Moderately alkaline |  |
|  | A15 | 8.3 | 24.2 | Moderately alkaline |  |
|  | A16 | 8.3 | 23.7 | Moderately alkaline |  |
|  | A17 | 8.6 | 23.6 | Strongly alkaline |  |
|  | A18 | 8.2 | 24.2 | Moderately alkaline |  |
|  | A19 | 8.5 | 23.9 | Strongly alkaline |  |
|  | A20 | 8.3 | 24.3 | Moderately alkaline |  |
|  | A21 | 8.4 | 23.9 | Moderately alkaline |  |

Table S5: Plasticity determination.

| Location | Samples | LL (%) | PL (%) | PI (%) | Characterization by Casagrande |
| --- | --- | --- | --- | --- | --- |
| Xi beach/Kefalonia | X10 | 40 | 22 | 18 | Clay of low plasticity |
|  | X11 | 46 | 26 | 20 | Clay of low plasticity |
|  | X12 | 47 | 27 | 20 | Clay of low plasticity |
|  | X13 | 50 | 28 | 22 | Clay of high plasticity |
|  | X14 | 50 | 30 | 20 | Clay of high plasticity |
|  | X15 | 45 | 25 | 20 | Clay of low plasticity |
|  | X16 | 52 | 28 | 24 | Clay of high plasticity |
|  | X17 | 41 | 22 | 20 | Clay of low plasticity |
|  | X18 | 37 | 20 | 17 | Clay of low plasticity |
|  | X19 | 31 | 19 | 12 | Clay of low plasticity |
|  | X21 | 31 | 20 | 12 | Clay of low plasticity |
|  | X22 | 43 | 24 | 18 | Clay of low plasticity |
|  | X23 | 28 | 21 | 7 | Silt of low plasticity |
|  | X24 | 44 | 24 | 20 | Clay of low plasticity |
|  | X25 | 40 | 22 | 17 | Clay of low plasticity |
|  | X26 | 36 | 22 | 14 | Clay of low plasticity |
|  | X27 | 35 | 21 | 14 | Clay of low plasticity |
|  | X28 | 29 | 23 | 6 | Silt of low plasticity |
|  | X29 | 49 | 23 | 26 | Clay of low plasticity |
|  | X30 | 31 | 21 | 10 | Clay of low plasticity |
|  | X31 | 38 | 26 | 12 | Silt of low plasticity |
|  | X32 | 34 | 22 | 11 | Clay of low plasticity |
|  | X33 | 41 | 25 | 16 | Clay of low plasticity |
|  | X34 | 78 | 16 | 62 | Clay of high plasticity |
|  | X35 | 32 | 23 | 9 | Silt/Clay of low plasticity |
|  | X36 | 47 | 26 | 22 | Clay of low plasticity |
|  | X37 | 27 | 21 | 6 | Silt/Clay of low plasticity |
|  | X38 | 30 | 21 | 8 | Clay of low plasticity |
|  | X39 | 31 | 24 | 7 | Silt of low plasticity |
|  | X40 | 30 | 23 | 7 | Silt of low plasticity |
|  | X41 | 37 | 27 | 10 | Silt of low plasticity |
|  | X42 | 41 | 29 | 12 | Silt of low plasticity |
|  | X43 | 40 | 28 | 11 | Silt of low plasticity |
|  | X44 | 36 | 26 | 9 | Silt of low plasticity |
|  | X45 | 38 | 27 | 12 | Silt of low plasticity |
|  | X46 | 33 | 28 | 5 | Silt of low plasticity |
|  | X47 | 41 | 20 | 21 | Clay of low plasticity |
|  | X48 | 39 | 27 | 12 | Silt of low plasticity |
|  | X49 | 38 | 19 | 19 | Clay of low plasticity |
|  | X50 | 49 | 25 | 23 | Clay of low plasticity |
|  | X51 | 42 | 29 | 13 | Silt of low plasticity |
|  | X53 | 44 | 25 | 19 | Clay of low plasticity |
| Koutala beach/Kefalonia | Κ0 | 41 | 21 | 20 | Clay of low plasticity |
|  | Κ1 | 38 | 30 | 8 | Silt of low plasticity |
|  | Κ3 | 48 | 22 | 25 | Clay of low plasticity |
|  | Κ4 | 46 | 11 | 35 | Clay of low plasticity |
|  | Κ5 | 60 | 15 | 44 | Clay of high plasticity |
|  | Κ6 | 48 | 46 | 1 | Silt of low plasticity |
|  | Κ8 | 40 | 18 | 21 | Clay of low plasticity |
| Matzavinata/Kefalonia | MA1 | 48 | 26 | 22 | Clay of low plasticity |
|  | MA2 | 43 | 22 | 21 | Clay of low plasticity |
|  | MA3 | 46 | 23 | 22 | Clay of low plasticity |
|  | MA4 | 46 | 23 | 22 | Clay of low plasticity |
|  | MA5 | 47 | 22 | 25 | Clay of low plasticity |
|  | MA6 | 49 | 17 | 26 | Clay of low plasticity |
|  | MA7 | 37 | 20 | 17 | Clay of low plasticity |
|  | MA8 | 41 | 23 | 18 | Clay of low plasticity |
|  | MA9 | 49 | 22 | 27 | Clay of low plasticity |
|  | MA10 | 54 | 26 | 28 | Clay of high plasticity |
|  | MA11 | 46 | 26 | 21 | Clay of low plasticity |
|  | MA12 | 40 | 24 | 16 | Clay of low plasticity |
|  | MA13 | 37 | 20 | 17 | Clay of low plasticity |
|  | MA14 | 40 | 22 | 17 | Clay of low plasticity |
|  | MA15 | 56 | 25 | 31 | Clay of high plasticity |
| Chavdata/Kefalonia | CH1 | 44 | 22 | 23 | Clay of low plasticity |
|  | CH2 | 41 | 23 | 18 | Clay of low plasticity |
|  | CH3 | 51 | 24 | 27 | Clay of high plasticity |
|  | CH4 | 46 | 24 | 22 | Clay of low plasticity |
|  | CH5 | 43 | 27 | 16 | Silt of low plasticity |
|  | CH6 | 41 | 18 | 23 | Clay of low plasticity |
|  | CH7 | 41 | 17 | 25 | Clay of low plasticity |
|  | CH8 | 48 | 20 | 27 | Clay of low plasticity |
|  | CH9 | 54 | 21 | 34 | Clay of high plasticity |
|  | CH10 | 47 | 23 | 25 | Clay of low plasticity |
|  | CH12 | 58 | 56 | 1 | Silt of high plasticity |
|  | CH14 | 48 | 23 | 25 | Clay of low plasticity |
|  | CH15 | 41 | 18 | 23 | Clay of low plasticity |
|  | CH17 | 40 | 17 | 23 | Clay of low plasticity |
|  | CH18 | 40 | 20 | 21 | Clay of low plasticity |
| Arillas beach/Corfu | B2 | 44 | 32 | 12 | Silt of low plasticity |
|  | B3 | 48 | 31 | 16 | Silt of low plasticity |
|  | B4 | 41 | 31 | 10 | Silt of low plasticity |
|  | B5 | 43 | 32 | 11 | Silt of low plasticity |
|  | B6 | 45 | 32 | 13 | Silt of low plasticity |
|  | B7 | 38 | 27 | 12 | Silt of low plasticity |
|  | B8 | 40 | 27 | 13 | Silt of low plasticity |
|  | B9 | 48 | 32 | 16 | Silt of low plasticity |
|  | B10 | 40 | 27 | 13 | Silt of low plasticity |
|  | B11 | 43 | 27 | 15 | Silt of low plasticity |
|  | B12 | 39 | 30 | 10 | Silt of low plasticity |
|  | B15 | 54 | 31 | 23 | Silt of high plasticity |
|  | B17 | 39 | 26 | 13 | Silt of low plasticity |
|  | B19 | 45 | 29 | 16 | Silt of low plasticity |
|  | B21 | 42 | 29 | 13 | Silt of low plasticity |
|  | B22 | 41 | 29 | 13 | Silt of low plasticity |
|  | B31 | 43 | 31 | 13 | Silt of low plasticity |
|  | B33 | 44 | 29 | 15 | Silt of low plasticity |
|  | B39 | 48 | 31 | 17 | Silt of low plasticity |
|  | B41 | 32 | 21 | 10 | Clay of low plasticity |
| Agios Stefanos beach/Corfu | Α0 | 45 | 23 | 22 | Clay of low plasticity |
|  | Α1 | 39 | 21 | 18 | Clay of low plasticity |
|  | Α2 | 46 | 28 | 18 | Clay of low plasticity |
|  | Α4 | 45 | 21 | 24 | Clay of low plasticity |
|  | Α5 | 40 | 21 | 19 | Clay of low plasticity |
|  | Α6 | 47 | 21 | 26 | Clay of low plasticity |
|  | Α7 | 48 | 19 | 29 | Clay of low plasticity |
|  | Α8 | 47 | 26 | 21 | Clay of low plasticity |
|  | Α9 | 47 | 24 | 23 | Clay of low plasticity |
|  | Α10 | 46 | 30 | 15 | Silt of low plasticity |
|  | Α11 | 44 | 28 | 16 | Silt of low plasticity |
|  | Α12 | 45 | 31 | 14 | Silt of low plasticity |
|  | Α13 | 46 | 29 | 17 | Silt of low plasticity |
|  | Α14 | 39 | 25 | 14 | Silt of low plasticity |
|  | Α15 | 46 | 30 | 16 | Silt of low plasticity |
|  | Α16 | 47 | 28 | 20 | Silt of low plasticity |
|  | Α17 | 47 | 29 | 18 | Silt of low plasticity |
|  | Α18 | 45 | 30 | 15 | Silt of low plasticity |
|  | Α19 | 52 | 31 | 21 | Silt of high plasticity |
|  | Α20 | 50 | 32 | 19 | Silt of high plasticity |

Table S6: Specific Surface Area Determination results.

| Location | Samples | Specific Surface (m2/gr) |
| --- | --- | --- |
| Xi beach/Kefalonia | X10 | 11 |
|  | X12 | 13 |
|  | X14 | 24 |
|  | X16 | 18 |
|  | X18 | 10 |
|  | X20 | 8 |
|  | X22 | 7 |
|  | X24 | 18 |
|  | X26 | 6 |
|  | X28 | 11 |
|  | X30 | 14 |
|  | X32 | 12 |
|  | X34 | 14 |
|  | X38 | 18 |
|  | X40 | 10 |
| Koutala beach/Kefalonia | Κ0 | 17 |
|  | Κ2 | 19 |
|  | Κ4 | 9 |
|  | Κ6 | 18 |
|  | Κ8 | 25 |
| Matzavinata/Kefalonia | ΜΑ1 | 9 |
|  | ΜΑ2 | 18 |
|  | ΜΑ3 | 19 |
|  | ΜΑ4 | 10 |
|  | ΜΑ5 | 14 |
|  | ΜΑ7 | 14 |
|  | ΜΑ8 | 15 |
|  | ΜΑ9 | 17 |
|  | ΜΑ10 | 14 |
|  | ΜΑ11 | 13 |
|  | ΜΑ12 | 12 |
|  | ΜΑ13 | 12 |
|  | ΜΑ14 | 14 |
|  | ΜΑ15 | 23 |
| Chavdata/Kefalonia | CH1 | 21 |
|  | CH2 | 19 |
|  | CH3 | 22 |
|  | CH4 | 20 |
|  | CH5 | 16 |
|  | CH6 | 22 |
|  | CH8 | 25 |
|  | CH9 | 25 |
|  | CH10 | 29 |
|  | CH12 | 25 |
|  | CH14 | 26 |
|  | CH15 | 19 |
|  | CH18 | 18 |
|  | CH42 | 20 |
|  | CH44 | 18 |
| Arillas beach/Corfu | Β2 | 18 |
|  | Β4 | 14 |
|  | Β6 | 14 |
|  | Β7 | 12 |
|  | Β9 | 14 |
|  | Β15 | 25 |
|  | Β17 | 20 |
|  | Β21 | 23 |
|  | Β22 | 13 |
|  | Β31 | 25 |
|  | Β33 | 15 |
|  | Β39 | 24 |
|  | Β40 | 9 |
| Agios Stefanos beach/Corfu | Α0 | 25 |
|  | Α2 | 25 |
|  | Α4 | 26 |
|  | Α5 | 17 |
|  | Α6 | 26 |
|  | Α7 | 24 |
|  | Α8 | 28 |
|  | Α9 | 20 |
|  | Α10 | 24 |
|  | Α11 | 24 |
|  | Α12 | 20 |
|  | Α13 | 24 |
|  | Α14 | 20 |
|  | Α15 | 15 |
|  | Α16 | 15 |
|  | Α17 | 14 |
|  | Α18 | 19 |
|  | Α19 | 19 |
|  | Α20 | 24 |